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	REGISTRO
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	04

	
	RECORD
	REVISION
	

	CODIGO | CODE
	SOLICITAÇÃO DE SERVIÇOS COMPLEMENTARES
	PÁGINA
	1/1

	IAS-RG-0103
	SUPPLEMENTARY REQUEST
	PAGE
	



	PN (PN):
	SN:
	Nº da OS (WO):
	TLN:02188

	        6791715
	B620
	IAS
	

	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	Serviço PrincipaL
(Main Service)
	QUANT:

	AE- 108636
	1- TUBE
	REVISÃO GERAL / OVERHAUL	1

	
	
	
	

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	1
	REPAIR SHOP	RETIFICA / RECTIFY	RETIFICAR A PONTA ASSINALADA ATÉ REMOVER TODO CROMO.
NÃO PRECISA ENCOSTAR A RETÍFICA NA FACE, PODE IR ATÉ 0.050¨ DA MESMA.

GRIND THE MARKED TIP UNTIL ALL CHROME IS REMOVED. YOU DON'T NEED TO TOUCH THE GRINDER TO THE FACE, IT CAN GO UP TO 0.050 ̈ FROM IT.

	2
	CHEMICAL CLEANING	DEPOSIÇÃO DE CROMO / CHROME PLATING	ISOLAR E APLICAR CROMO DURO NO DIÂMETRO RETIFICADO.
APÓS RETÍFICA FINAL FICARÁ 0.499¨

ISOLATE AND APPLY HARD CHROME TO THE GROUND DIAMETER. AFTER FINAL RECTIFICATION IT WILL BE 0.499

	3
	CHEMICAL CLEANING	TRATAMENTO TERMICO / HEAT TREATMENT	TRATAMENTO TÉRMICO EM 190° C POR 3 HORAS.

HEAT TREATMENT AT 190° C FOR 3 HOURS.

	4
	REPAIR SHOP	RETIFICA / RECTIFY	RETIFICAR O DIÂMETRO CROMADO, CENTRAR PELO INTERNO, DEIXANDO= 0.499¨- 0.0003¨
REMOVER CANTO VIVO.

GRIND THE CHROME DIAMETER, CENTER FROM THE INSIDE, ALLOWING= 0.499 ̈-0.0003 ̈ REMOVE LIVE CORNER.

	5
	NDT	END- PARTICULAS MAGNETICAS / NOT - MAGNETIC PARTICLE	EXECUTAR MPI: ASTM E 1444.
APRESENTOU INDICAÇÃO? (  )SIM   (  )NÃO

RUN MPI: ASTM E 1444. DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	6
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	7
	T56A	INSPEÇÃO / INSPECTION	INSPEÇÃO FINAL.
(  )APROVADO     (  )REPROVADO

FINAL INSPECTION. ( )APPROVED ( )FAILED

	
	Escolher um item.	Escolher um item.	

	
	Escolher um item.	Escolher um item.	

	
	
	
	

	
	
	
	

	
	
	
	

	
	
	
	

	OBSERVAÇÕES
(Observation):
	ASSINATURA DO SOLICITANTE 
(Signature):
	DATA 28/10/2025
(Date):

	[bookmark: Texto2]     
	VILSON BARBOSA
	28/10/2025


· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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