| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN:02188 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 23064894 |  |  | 25516 |  |  |  |  | IAS |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| AE-109692 |  |  |  | TU. VANE 4º ST |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | REMOVER OS SEALS CONFORME A IP-0006, 3.8 REMOVE SEALS IN ACCORDANCE WITH IP-0006, 3.8 |  |  |  |  |  |  |
| 2 | NDT | END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION |  |  | EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL-3. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN FPI: ASTM E 1417, METHOD-A, LEVEL-3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 3 | CHEMICAL CLEANING | JATEAR / BLAST |  |  | LIMPAR COM GLASS BEAD BAIXA PRESSÃO. IP-0006,3.26 CLEAN WITH LOW PRESSURE GLASS BEAD. IP-0006,3.26 |  |  |  |  |  |  |
| 4 | CHEMICAL CLEANING | DEPOSIÇÃO DE NIQUEL-CADMIO / NICKEL-CADMIUM PLATING |  |  | APLICAR NICKEL CÁDMIO, CONFORME AMS 2416. APPLY NICKEL CADMIUM IN ACCORDANCE WITH AMS 2416. |  |  |  |  |  |  |
| 5 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | APERTAR AS ALHETAS NO OUTER RING, REMANCHANDO A PONTA ADJACENTE AOS 5 FUROS. TIGHTEN THE FINS IN THE OUTER RING, STAINING THE TIP ADJACENT TO THE 5 HOLES. |  |  |  |  |  |  |
| 6 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | INSTALAR OS NOVOS SEALS CONFORME A IT-0051. INSTALL THE NEW SEALS ACCORDING TO IT-0051. |  |  |  |  |  |  |
| 7 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 29/10/2025 (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 29/10/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)