| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN:02188 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6845945 |  |  | 17322 |  |  |  |  | IAS |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| AE- 109008 |  |  |  | TIE BOLT |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | REPAIR SHOP | RETIFICA / RECTIFY |  |  | RETIFICAR O DIÂMETRO DO RESALTO- 9º ST, ATÉ REMOVER O CROMO. RECTIFY THE DIAMETER OF THE SHOULDER - 9TH ST, UNTIL THE CHROME IS REMOVED. |  |  |  |  |  |  |
| 2 | CHEMICAL CLEANING | DEPOSIÇÃO DE CROMO / CHROME PLATING |  |  | ISOLAR E APLICAR CROMO DURO NO DIÂMETRO EXTERNO 9º ST, QUE FICARÁ APÓS RETÍFICA FINAL COM 0.8750¨ ISOLATE AND APPLY HARD CHROME ON THE EXTERNAL DIAMETER 9º ST, WHICH WILL REMAIN AFTER FINAL GRINDING WITH 0.8750 |  |  |  |  |  |  |
| 3 | CHEMICAL CLEANING | TRATAMENTO TERMICO / HEAT TREATMENT |  |  | TRATAMENTO TÉRMICO EM 190° C POR 3- HORAS. HEAT TREATMENT AT 190° C FOR 3-HOURS. |  |  |  |  |  |  |
| 4 | REPAIR SHOP | RETIFICA / RECTIFY |  |  | RETIFICAR O DIÂMETRO CROMADO, DEIXANDO COM 0.8750¨- 0.0002¨ REMOVER OS CANTOS VIVOS. RECTIFY THE CHROME DIAMETER, LEAVING IT WITH 0.8750 ̈- 0.0002 ̈ REMOVE SHARP CORNERS. |  |  |  |  |  |  |
| 5 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | REMOVER E SUAVISAR OS EXCESSOS DE CROMO DOS REBAIXOS DO DIÂMETRO 9º ST RETIFICADO. REMOVE AND SMOOTH EXCESS CHROME FROM THE RECESSES OF THE 9º ST RECTIFIED DIAMETER. |  |  |  |  |  |  |
| 6 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 7 | NDT | END- PARTICULAS MAGNETICAS / NOT - MAGNETIC PARTICLE |  |  | EXECUTAR MPI: ASTM E 1444. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN MPI: ASTM E 1444. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 8 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 9 | CHEMICAL CLEANING | FOSFATIZAÇÃO / PHOSPHATIZATION |  |  | APLICAR PHOSPHATE COATING- AMS 2481 NA ROSCA E NA CABEÇA. APPLY PHOSPHATE COATING- AMS 2481 TO THE THREAD AND HEAD. |  |  |  |  |  |  |
| 10 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 11/11/2025 (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 11/11/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)