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	SOLICITAÇÃO DE SERVIÇOS COMPLEMENTARES
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	PN (PN):
	SN:
	Nº da OS (WO):
	TLN:02188

	                         6850825
	N/C
	IAS
	

	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	Serviço PrincipaL
(Main Service)
	QUANT:

	AE- 109008
	DRIVE GEAR
	REVISÃO GERAL / OVERHAUL	1

	
	
	
	

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	1
	REPAIR SHOP	RETIFICA / RECTIFY	RETIFICAR O DIÂMETRO ¨AR¨, DEIXANDO COM 0.494¨ +ou- 0.001¨
NOTA: NÃO APROXIME DOS DENTES MENOS QUE 0.060¨

RECTIFY THE DIAMETER OF THE AIR, LEAVING IT WITH 0.494 ̈ + OR- 0.001 ̈ NOTE: DO NOT APPROACH THE TEETH LESS THAN 0.060

	2
	CHEMICAL CLEANING	DEPOSIÇÃO DE CROMO / CHROME PLATING	ISOLAR E APLICAR CROMO DURO NO DIÂMETRO ¨AR¨, QUE SERÁ APÓS RETÍFICA FINAL 0.4987¨

ISOLATE AND APPLY HARD CHROME IN THE DIAMETER ̈AR ̈, WHICH WILL BE AFTER FINAL GRINDING 0.4987

	3
	CHEMICAL CLEANING	TRATAMENTO TERMICO / HEAT TREATMENT	TRATAMENTO TÉRMICO EM 190° C POR 3- HORAS.

HEAT TREATMENT AT 190° C FOR 3-HOURS.

	4
	REPAIR SHOP	RETIFICA / RECTIFY	RETIFICAR O DIÂMETRO CROMADO, DEIXANDO COM 0.4987¨+ou- 0.0002¨
REMOVER CANTO VIVO.

RECTIFY THE CHROME DIAMETER, LEAVING IT WITH 0.4987 ̈+or- 0.0002 ̈ REMOVE LIVE CORNER.

	5
	CHEMICAL CLEANING	LIMPAR / CLEAN	           LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	6
	NDT	END- PARTICULAS MAGNETICAS / NOT - MAGNETIC PARTICLE	EXECUTAR MPI: ASTM E 1444.
APRESENTOU INDICAÇÃO? (  )SIM   (  )NÃO

RUN MPI: ASTM E 1444. DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	7
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	8
	T56A	INSPEÇÃO / INSPECTION	INSPEÇÃO FINAL.
(  )APROVADO    (  )REPROVADO

FINAL INSPECTION. ( )APPROVED ( )FAILED

	
	Escolher um item.	Escolher um item.	

	
	
	
	

	
	
	
	

	
	
	
	

	
	
	
	

	OBSERVAÇÕES
(Observation):
	ASSINATURA DO SOLICITANTE 
(Signature):
	DATA 11/11/2025
(Date):

	[bookmark: Texto2]     
	VILSON BARBOSA
	11/11/2025


· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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