| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN:02188 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6792269 |  |  | H527 |  |  |  |  | IAS |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| AE- 109008 |  |  |  | PUMP COVER |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 2 | CHEMICAL CLEANING | DECAPAGEM / STRIPPING |  |  | DECAPAR A TINTA, IP-0006, 3.18 INK STRIPPING, IP-0006, 3.18 |  |  |  |  |  |  |
| 3 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR O FURO NA FACE-G, CENTRANDO PELO PRÓPRIO E DEIXANDO: O DIÂMETRO INTERNO= 0.5145¨ +ou- 0.0002¨ PROFUNDIDADE= 0.360¨+ou-0.0002¨ MACHINE THE HOLE ON THE G-FACE, CENTERING IT ON ITS OWN AND LEAVING: INNER DIAMETER= 0.5145 ̈ +or- 0.0002 ̈ DEPTH= 0.360 ̈+or-0.0002 |  |  |  |  |  |  |
| 4 | REPAIR SHOP | USINAGEM / MACHINING |  |  | CONFECCIONAR 1- BUCHA DE BROZE: COM APERTO NA TAMPA= 0.001¨-0.0005¨ PROFUNDIDADE= 0.358¨ DIÂMETRO INTERNO=0.4365¨+0.0005¨ MAKE 1- BROZE BUSHING: WITH TIGHTENING ON LID= 0.001 ̈-0.0005 ̈ DEPTH= 0.358 ̈ INNER DIAMETER=0.4365 ̈+0.0005 |  |  |  |  |  |  |
| 5 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | CONFERIR E MARCAR NA FACE-G, A POSIÇÃO DO PINO P/N=MS9486-56 VEJA A INCLINAÇÃO DO MESMO NA FIGURA ANEXA. MONTAR A BUCHA NOVA e INSTALAR ESTE PINO OBLIQUO. NOTA: ANTES DE PINAR PEDIR NA INSPEÇÃO O EIXO PARA VERIFICAR SE ESTÁ ENTRANDO NA BUCHA. CHECK AND MARK ON THE G-FACE, THE POSITION OF THE PIN P/N=MS9486-56 SEE THE INCLINATION OF THE SAME IN THE ATTACHED FIGURE. MOUNT THE NEW BUSHING and INSTALL THIS OBLIQUE PIN. NOTE: BEFORE PINNING, ASK FOR THE AXLE INSPECTION TO CHECK IF IT IS ENTERING THE BUSHING. |  |  |  |  |  |  |
| 6 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 7 | NDT | END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION |  |  | EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL-3. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN FPI: ASTM E 1417, METHOD-A, LEVEL-3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 8 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 9 | REPAIR SHOP | ISOLAÇÃO / MASK |  |  | ISOLAR OS PRISIONEIROS, FUROS E AS ÁREAS DE CONTATO. ISOLATE STUDS, HOLES, AND CONTACT AREAS. |  |  |  |  |  |  |
| 10 | REPAIR SHOP | PINTURA / PAINTING |  |  | PINTAR EXTERNAMENTE COM: PRIMER PA-0060 e CINZA PA-0065. PAINT EXTERNALLY WITH: PRIMER PA-0060 and GRAY PA-0065. |  |  |  |  |  |  |
| 11 | REPAIR SHOP | REMOVER ISOLAMENTO / REMOVE MASK |  |  | REMOVER AS ISOLAÇÕES E OS EXCESSOS DE TINTA. REMOVE INSULATION AND EXCESS PAINT. |  |  |  |  |  |  |
| 12 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 13/11/2025 (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 13/11/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)