| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN:02188 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6850825 |  |  | N/C |  |  |  |  | IAS |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| AE- 109692 |  |  |  | 3- SHAFT GEARS |  |  | REVISÃO GERAL / OVERHAUL |  | 3 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | REPAIR SHOP | RETIFICA / RECTIFY |  |  | RETIFICAR O DIÂMETRO -AR, DEIXANDO COM 0.493¨-0.002¨ NÃO APROXIMAR DOS DENTES A RETÍFICA, MENOS QUE 0.060¨ NOTA: O QUE ESTIVER MENOR, APENAS POLIR. VEJA A FIGURA ANEXA. RECTIFY THE -AR DIAMETER, LEAVING 0.493 ̈-0.002 ̈ DO NOT BRING THE GRINDING MACHINE CLOSER TO THE TEETH, LESS THAN 0.060 ̈ NOTE: WHICHEVER IS SMALLER, JUST POLISH. SEE THE ATTACHED FIGURE. |  |  |  |  |  |  |
| 2 | CHEMICAL CLEANING | DEPOSIÇÃO DE CROMO / CHROME PLATING |  |  | ISOLAR E APLICAR CROMO DURO NO DIÂMETRO -AR, QUE APÓS A RETÍFICA FINAL FICARÁ COM 0.4985¨ ISOLATE AND APPLY HARD CHROME IN THE AR DIAMETER, WHICH AFTER THE FINAL GRINDING WILL BE 0.4985 |  |  |  |  |  |  |
| 3 | CHEMICAL CLEANING | TRATAMENTO TERMICO / HEAT TREATMENT |  |  | TRATAMENTO TÉRMICO EM 190° C POR 3- HORAS. HEAT TREATMENT AT 190° C FOR 3-HOURS. |  |  |  |  |  |  |
| 4 | REPAIR SHOP | RETIFICA / RECTIFY |  |  | RETIFICAR O CROMO, DEIXANDO O DIÂMETRO= 0.4985¨-0.0002¨ REMOVER OS CANTOS VIVOS. RECTIFY THE CHROME, LEAVING THE DIAMETER= 0.4985 ̈-0.0002 ̈ REMOVE SHARP CORNERS. |  |  |  |  |  |  |
| 5 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 6 | NDT | END- PARTICULAS MAGNETICAS / NOT - MAGNETIC PARTICLE |  |  | EXECUTAR MPI: ASTM E 1444. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN MPI: ASTM E 1444. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 7 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 8 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 18/11/2025 (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 18/11/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)