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	REGISTRO
	REVISÃO
	04

	
	RECORD
	REVISION
	

	CODIGO | CODE
	SOLICITAÇÃO DE SERVIÇOS COMPLEMENTARES
	PÁGINA
	1/1

	IAS-RG-0103
	SUPPLEMENTARY REQUEST
	PAGE
	



	PN (PN):
	SN:
	Nº da OS (WO):
	TLN:

	    RR30000160  
	YP11076
	051806
	02027

	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	Serviço PrincipaL
(Main Service)
	QUANT:

	RRE-200321
	HOUSING ASSY, GEARBOX
	REPARO / REPAIR	01

	     
	     
	TSO:                    
	CSO:      

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	Remover corrosão nas superfícies externas, aplicar epoxy preenchendo os defeitos causados pela corrosão deixando o perfil o mais próximo do original possível 

Remove corrosion on external surfaces, apply epoxy filling defects caused by corrosion, leaving the profile as close to the original as possible.


	
	CHEMICAL CLEANING	LIMPAR / CLEAN	Realizar limpeza da peça conforme IAS-IP-0006 item 3.34 rev.3.

Perform Cleaning iaw IAS-IP-0006 item 3.34 rev.3.



	
	CHEMICAL CLEANING	APLICAR / APPLY	Aplique a solução de dicromato no metal base exposto.

Apply the dichromate solution to the bare metal.



	
	REPAIR SHOP	PINTURA / PAINTING	MASCARAMENTO:

Isolar os prisioneiros, HELICOILS, faces de assentamento, PN e SN e locais onde não será aplicado coating. (task 70-32-11-300-801 – application of corrosion resistant paint)

MASKING:

Insolate studs, HELICOILS, seating faces, PN and SN and places where no coating will be applied. (task 70-32-11-300-801 - application of corrosion resistant paint).



	
	REPAIR SHOP	PINTURA / PAINTING	Realizar pintura conforme IAS-IP-0005 Item 3.13 Rev.05 (task 70-32-11-300-801 – application of corrosion resistant paint).

Apply coating per IAS-IP-0005 Item 3.13 Rev.05 (task 70-32-11-300-801 – application of corrosion resistant paint).


	
	CHEMICAL CLEANING	LIMPAR / CLEAN	Proteger o componente lubrificando todas as gaiolas de localização dos rolamentos, prisioneiros e inserts.

Protect the component by lubricating all bearing location cages, studs and inserts.



	
	RR300	INSPEÇÃO / INSPECTION	Inspeção final

Final inspection.



	     
	Escolher um item.	Escolher um item.	     

	     
	Escolher um item.	Escolher um item.	     
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	Escolher um item.	Escolher um item.	     

	     
	Escolher um item.	Escolher um item.	     

	     
	Escolher um item.	Escolher um item.	     
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	Escolher um item.	Escolher um item.	     

	     
	Escolher um item.	Escolher um item.	     

	OBSERVAÇÕES
(Observation):
	ASSINATURA DO SOLICITANTE 
(Signature):
	DATA 
(Date):

	[bookmark: Texto2]     
	ANTONIO CLAUDIO
	11/03/2026


· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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