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	REGISTRO
	REVISÃO
	04

	
	RECORD
	REVISION
	

	CODIGO | CODE
	SOLICITAÇÃO DE SERVIÇOS COMPLEMENTARES
	PÁGINA
	1/1

	IAS-RG-0103
	SUPPLEMENTARY REQUEST
	PAGE
	



	PN (PN):
	SN:
	Nº da OS (WO):
	TLN:

	23052265
	DW36967
	050541
	

	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	Serviço PrincipaL
(Main Service)
	QUANT:

	CAE-280068
	GAS PRODUCER TURBINE SUPPORT
	REPARO / REPAIR	1

	TSN:
	CSN:
	TSO:
	CSO:

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	01
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	Realizar blend da área trincada até o final da trinca mantendo acabamento conforme perfil original.

Blend the cracked area all the way to the end of the crack, maintaining a finish that matches the original profile.

	02
	CHEMICAL CLEANING	NON-DESTRUCTIVE TESTING	Realizar NDT no local trabalhado  conforme indicado no Overhaul Manual 16W3.
Perform NDT on the site worked as indicated in the Overhaul Manual 16W3.
Ensaio (Test): FPI
Tipo (Type): 1
Método (Method): A
Sensibilidade (Sensitivity): 2
                 
Foram encontradas indicações?
(Were Indications found?)

( ) SIM – REGISTRAR IAS-RG-0332.
         YES – REGISTRAR IAS-RG-0332.

( ) NÃO – PROCESSEGUIR PARA ETAPA DE LIMPEZA PÓS NDT
           NO – PROCEED TO THE AFTER NDT CLEANING STEP.

	03
	M250	INSPEÇÃO / INSPECTION	Realizar inspeção pós NDT do item.

Perform post-NDT inspection.

	04
	CHEMICAL CLEANING	LIMPAR / CLEAN	Realizar limpeza pós NDT conforme IAS IP-006 item 3.34.

Perform post-NDT clean according to IAS IP-006 item 3.34

	05
	CHEMICAL CLEANING	JATEAR / BLAST	Realizar jateamento do componente conforme IAS IP-006 item 3.26.

Perform component blasting according to IAS IP-006 item 3.26.

	06
	CHEMICAL CLEANING	LIMPAR / CLEAN	Realizar limpeza do componente conforme IAS IP-006 item 3.30

Perform componente cleanig according to IAS IP-006 item 3.30

	07
	ACESSÓRIOS	APROVAÇÃO FINAL DO SERVLÇO REALIZADO / FINAL APPROVAL OF THE SERVICE	Realizar inspeção final dos serviços realizados.

Perform final inspection of the work performed.

	OBSERVAÇÕES
(Observation):
	ASSINATURA DO SOLICITANTE 
(Signature):
	DATA 
(Date):

	[bookmark: Texto2]     
	MATEUS MACHADO
	20/03/2026


· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)


	




image1.png




