| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN - 02623 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 23052067 |  |  | JJ00511 |  |  |  |  | 052065 |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| CAG-650070 |  |  |  | REAR PINION BEARING INNER RACE |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 2 | NDT | END- PARTICULAS MAGNETICAS / NOT - MAGNETIC PARTICLE |  |  | EXECUTAR MPI, CONFORME ASTM E 1444. APRESENTOU INDICAÇÃO? ( ) SIM ( ) NÃO PERFORM MPI, AS PER ASTM AND 1444. DID YOU PRESENT AN INDICATION? ( ) YES ( ) NO |  |  |  |  |  |  |
| 3 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 4 | CHEMICAL CLEANING | DEPOSIÇÃO DE PRATA/ SILVER PLATING |  |  | ISOLAR E APLICAR 0.0007¨DE ESPESSURA DE COBRE NO DIÂMETRO INTERNO. AMS 2400 NOTA: MUITO CUIDADO PARA NÃO ATACAR A PISTA EXTERNA POIS É DE ROLAMENTO. ISOLATE AND APPLY 0.0007 ̈OF COPPER THICKNESS TO THE INNER DIAMETER. AMS 2400 NOTE: BE VERY CAREFUL NOT TO ATTACK THE OUTER TRACK AS IT IS A ROLLING TRACK. |  |  |  |  |  |  |
| 5 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( ) APROVADO ( )REPROVADO INAL INSPECTION. ( ) APPROVED ( )FAILED |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 23/04/2026 (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 23/04/2026 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)