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	PN (PN):
	SN:
	Nº da OS (WO):
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	            6871447
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	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	Serviço PrincipaL
(Main Service)
	QUANT:

	CAE-550367
	           COMPRESSOR CASE 
	REVISÃO GERAL / OVERHAUL	1

	
	
	
	

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	1
	REPAIR SHOP	USINAGEM / MACHINING	USINAR OS 14- DIÂMETROS INTERNOS ATÉ REMOVER TODO MATERIAL BASE.

MACHINE THE 14- INTERNAL DIAMETERS UNTIL ALL BASE MATERIAL IS REMOVED.

	2
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	REMOVER OS PARAFUSOS DE UNIÃO , PARA SEPARAR EM 2- METADES.

REMOVE THE BOLTS OF UNION, TO SEPARATE INTO 2-HALVES.

	3
	CHEMICAL CLEANING	REPAROS MANUAIS / MANUAL REPAIR	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	4
	NDT	END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION	EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL-3.
APRESENTOU INDICAÇÃO?  (  )SIM   (  )NÃO

RUN FPI: ASTM E 1417, METHOD-A, LEVEL-3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	5
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	6
	REPAIR SHOP	PINTURA / PAINTING	ISOLAR E APLICAR EXTERNAMENTE SERMETEL W ou ALSEAL 500., IP-0006, 3.17

ISOLATE AND APPLY EXTERNALLY SERMETEL 518, IP-0006, 3.17

	7
	REPAIR SHOP	METALIZAÇÃO / THERMAL SPRAY	METALIZAR INTERNAMENTE COM ALUMÍNIO.

INTERNALLY METALLIZE WITH ALUMINUM.

	8
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	LIMPAR AS FACES E UNIR AS 2- METADES.

CLEAN THE FACES AND JOIN THE 2- HALVES.

	9
	REPAIR SHOP	USINAGEM / MACHINING	USINAR AS CANALETAS, REMOVENDO O ALUMÍNIO E DEIXANDO NAS MEDIDAS DA FIGURA DA PÁGINA-924 ANEXA.

MACHINE THE GUTTERS, REMOVING THE ALUMINUM AND LEAVING IT IN THE MEASUREMENTS OF THE FIGURE ON PAGE-924 ATTACHED.

	10
	REPAIR SHOP	USINAGEM / MACHINING	CENTRAR PELOS DIÂMETROS INTERNOS, QUE ALOJAM AS VANES DAS EXTREMIDADES.
USINAR O DIÂMETRO DOS 14- RESALTOS INTERNOS, DEIXANDO:
DO 1º ao 9º ST= 14. 726¨ +ou- 0.001¨
e DO 10º ao 14º ST= 14.732¨+ou- 0.001¨
VEJA A FIGURA DA PÁGINA 923 ANEXA.



	11
	REPAIR SHOP	USINAGEM / MACHINING	USINAR OS 3- TIPOS DE CHANFROS, CONFORME AS MEDIDAS DA FIGURA DA PÁGINA 923 ANEXA.
MACHINE THE 3- TYPES OF CHAMFERS, ACCORDING TO THE MEASUREMENTS OF THE FIGURE ON PAGE 923 ATTACHED.


	12
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	SUAVISAR AS ÁREAS USINADAS, REMOVENDO OS EXCESSOS DE ALUMÍNIO.

SMOOTH THE MACHINED AREAS, REMOVING EXCESS ALUMINUM.

	13
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	LIMPAR E POLIR AS ROSCAS E FACES DE CONTATO.

CLEAN AND POLISH THE THREADS AND CONTACT FACES.

	14
	T56A	MONTAG EM/ ASSEMBLY	MONTAR AS VANES, CONFORME AS MEDIDAS DA PÁGINA 924 ANEXA.

ASSEMBLE THE VANES, ACCORDING TO THE MEASUREMENTS ON PAGE 924 ATTACHED.

	15
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	AJUSTAR AS PONTAS DOS ARCOS DA VANES, REMOVENTO O QUE EXCEDER DAS FACES DAS METADES.

ADJUST THE TIPS OF THE VANES ARCHES, REMOVING WHAT EXCEEDS THE FACES OF THE HALVES.

	16
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	LIMPAR AS FACES E UNIR AS 2- METADES COM VÁRIOS PARAFUSOS.

CLEAN THE FACES AND JOIN THE 2- HALVES WITH SEVERAL SCREWS.

	17
	REPAIR SHOP	USINAGEM / MACHINING	USINAR OS DIÂMETROS INTERNOS DOS SEALS DAS VANES, CONFORME A TABELA DA PÁGINA 405 ANEXA.

MACHINE THE INTERNAL DIAMETERS OF THE SEALS OF THE VANES, ACCORDING TO THE TABLE ON PAGE 405 ATTACHED.

	18
	CHEMICAL CLEANING	LIMPAR / CLEAN	LAVAR CONFORME A IP-0006, 3.10

WASH ACCORDING TO IP-0006, 3.10

	19
	T56A	INSPEÇÃO / INSPECTION	INSPEÇÃO FINAL.
(  ) APROVADO    (  )REPROVADO

FINAL INSPECTION. ( ) APPROVED ( )FAILED
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(Observation):
	ASSINATURA DO SOLICITANTE 
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	VILSON BARBOSA
	29/04/2026


· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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