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	REVISION
	

	CODIGO | CODE
	SOLICITAÇÃO DE SERVIÇOS COMPLEMENTARES
	PÁGINA
	1/1

	IAS-RG-0103
	SUPPLEMENTARY REQUEST
	PAGE
	



	PN (PN):
	SN:
	Nº da OS (WO):
	TLN:

	6894068
	MH136267
	052061
	02623

	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	Serviço PrincipaL
(Main Service)
	QUANT:

	TU-750638
	COMBUSTION LINER
	REVISÃO GERAL / OVERHAUL	01

	     
	     
	TSO:                    
	CSO:      

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	01
	REPAIR SHOP	TRATAMENTO TERMICO / HEAT TREATMENT	EXECUTAR TRATAMENTO TÉRMICO EM 1010°C, POR 30 MINUTOS.

PERFORM HEAT TREATMENT AT 1010°C FOR 30 MINUTES.

	02
	REPAIR SHOP	SOLDAR / WELDING	PREPARAR E SOLDAR 03 TRINCAS EXTERNAS NA AREA DE ESCAPE, MARCADAS NA PEÇA.  AMS-5798
SUAVISAR AS SOLDAS. TASK 72-47-00-300-801

PREPARE AND WELD THREE (03) EXTERNAL CRACKS LOCATED IN THE EXHAUST AREA, AS IDENTIFIED ON THE PART, IN ACCORDANCE WITH AMS 5798.
BLEND/SMOOTH THE WELDS TO ENSURE PROPER SURFACE FINISH.
PERFORM THE TASK IN ACCORDANCE WITH TASK 72-47-00-300-801

	03
	REPAIR SHOP	TRATAMENTO TERMICO / HEAT TREATMENT	EXECUTAR TRATAMENTO TÉRMICO EM 1010°C, POR 30 MINUTOS.

PERFORM HEAT TREATMENT AT 1010°C FOR 30 MINUTES.

	04
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	-CALIBRAR: 
AS 6- DEFLETORAS INTERNAS
A ÁREA DE ESCAPE
E OS CORRUGADOS.

CALIBRATE: 
THE 6- INTERNAL DEFLECTORS
THE ESCAPE AREA
AND THE CORRUGATED.

	05
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	06
	NDT	END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION	EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL 3.
APRESENTOU INDICAÇÃO? (  )SIM          (  )NÃO

RUN FPI: ASTM E 1417, METHOD-A, LEVEL 3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	07
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	08
	T56A	INSPEÇÃO / INSPECTION	INSPEÇÃO FINAL.
(  )APROVADO               (  )REPROVADO

FINAL INSPECTION. ( )APPROVED ( )FAILED
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· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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