| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN: 02623 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6876496 |  |  | A-5674 |  |  |  |  | 052062 |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| CAE-550367 |  |  |  | DIFFUSER |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | CORTAR E SUAVISAR OS PONTOS INTERNOS DE SOLDA, QUE PRENDEM A BAFFLE. CUT AND SMOOTH THE INTERNAL WELDING POINTS, WHICH HOLD THE BAFFLE. |  |  |  |  |  |  |
| 2 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | ESCOVAR E PASSAR AR COMPRIMIDO NA ÁREA INTERNA ONDE A BAFFLE COBRIA. BRUSH AND PASS COMPRESSED AIR ON THE INTERNAL AREA WHERE THE BAFFLE WAS COVERED. |  |  |  |  |  |  |
| 3 | REPAIR SHOP | SOLDAR / WELDING |  |  | INSTALAR A BAFFLE P/N= 6874445, COM PONTOS DE SOLDA: AMS 5776 ou (AMS 5680, AMS 5782, AMS 5784) INSTALLING THE BAFFLE P/N= 6874445, WITH WELD POINTS: AMS 5776 or (AMS 5680, AMS 5782, AMS 5784) |  |  |  |  |  |  |
| 4 | REPAIR SHOP | ISOLAÇÃO / MASK |  |  | ISOLAR AS ROSCAS, DIÂMETROS E AS ÁREAS DE CONTATO. ISOLATE THE THREADS, DIAMETERS AND CONTACT AREAS. |  |  |  |  |  |  |
| 5 | REPAIR SHOP | PINTURA / PAINTING |  |  | APLICAR SERMETEL-518 EXTERNAMENTE, CONFORME A IP-0006, 3.17 APPLY SERMETEL-518 EXTERNALLY, CONFORMING TO IP-0006, 3.17 |  |  |  |  |  |  |
| 6 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | REMOVER OS PINOS E A SLEEVE LIMPAR AS ÁREAS DE CONTATO E REINSTALAR A MESMA. NOTA: NÃO FRENAR ANTES DO TESTE DE PRESSÃO. REMOVING THE PINS AND SLEEVE CLEANING THE CONTACT AREAS AND REINSTALL IT. NOTE: DO NOT BRAKE BEFORE THE PRESSURE TEST. |  |  |  |  |  |  |
| 7 | T56A | INSPEÇÃO / INSPECTION |  |  | TESTE DE PRESSÃO NO SUMP. PRESSURE TEST ON SUMP. |  |  |  |  |  |  |
| 8 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | FRENAR A SLEEVE COM 2- PINOS P/N= 6739977. FRENAR A SLEEVE COM 2- PINOS P/N= 6739977. |  |  |  |  |  |  |
| 9 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | POLIR O DIÂMETRO INTERNO DO CAGE, ATÉ ACENTAR A PISTA NA BASE. POLISH THE INNER DIAMETER OF THE CAGE, UNTIL THE TRACK IS AT THE BASE. |  |  |  |  |  |  |
| 10 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | POLIR AS ROSCAS, DIÂMETROS E TODAS ÁREAS DE CONTATO. POLISHING THE THREADS, DIAMETERS AND ALL CONTACT AREAS |  |  |  |  |  |  |
| 11 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LAVAR AS ÁREAS POLIDAS, INTERNAMENTE E AS VIAS COM JATOS DE PRESSÃO, IP-0006, 3.10 WASHING POLISHED AREAS, INTERNALLY AND VIAS WITH PRESSURE JETS, IP-0006, 3.10 |  |  |  |  |  |  |
| 12 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. FINAL INSPECTION. |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 12/05/2026 (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 12/05/2026 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)