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(Description)

	1
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	CORTAR E SUAVISAR OS PONTOS INTERNOS DE SOLDA, QUE PRENDEM A BAFFLE.

CUT AND SMOOTH THE INTERNAL WELDING POINTS, WHICH HOLD THE BAFFLE.

	2
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	ESCOVAR E PASSAR AR COMPRIMIDO NA ÁREA INTERNA ONDE A BAFFLE COBRIA.

BRUSH AND PASS COMPRESSED AIR ON THE INTERNAL AREA WHERE THE BAFFLE WAS COVERED.

	3
	REPAIR SHOP	SOLDAR / WELDING	INSTALAR A BAFFLE P/N= 6874445, COM PONTOS DE SOLDA: AMS 5776 ou (AMS 5680, AMS 5782, AMS 5784)

INSTALLING THE BAFFLE P/N= 6874445, WITH WELD POINTS: AMS 5776 or (AMS 5680, AMS 5782, AMS 5784)

	4
	REPAIR SHOP	ISOLAÇÃO / MASK	ISOLAR AS ROSCAS, DIÂMETROS E AS ÁREAS DE CONTATO.
ISOLATE THE THREADS, DIAMETERS AND CONTACT AREAS.

	5
	REPAIR SHOP	PINTURA / PAINTING	APLICAR SERMETEL-518 EXTERNAMENTE, CONFORME A IP-0006, 3.17
 APPLY SERMETEL-518 EXTERNALLY, CONFORMING TO IP-0006, 3.17

	6
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	REMOVER OS PINOS E A SLEEVE
LIMPAR AS ÁREAS DE CONTATO
E REINSTALAR A MESMA.
NOTA: NÃO FRENAR ANTES DO TESTE DE PRESSÃO.

REMOVING THE PINS AND SLEEVE CLEANING THE CONTACT AREAS AND REINSTALL IT. NOTE: DO NOT BRAKE BEFORE THE PRESSURE TEST.

	7
	T56A	INSPEÇÃO / INSPECTION	TESTE DE PRESSÃO NO SUMP.

PRESSURE TEST ON SUMP.

	8
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	FRENAR A SLEEVE COM 2- PINOS P/N= 6739977.

FRENAR A SLEEVE COM 2- PINOS P/N= 6739977.

	9
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	POLIR O DIÂMETRO INTERNO DO CAGE, ATÉ ACENTAR A PISTA NA BASE.

POLISH THE INNER DIAMETER OF THE CAGE, UNTIL THE TRACK IS AT THE BASE.

	10
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	POLIR AS ROSCAS, DIÂMETROS E TODAS ÁREAS DE CONTATO.

POLISHING THE THREADS, DIAMETERS AND ALL CONTACT AREAS

	11
	CHEMICAL CLEANING	LIMPAR / CLEAN	LAVAR AS ÁREAS POLIDAS, INTERNAMENTE E AS VIAS COM JATOS DE PRESSÃO, IP-0006, 3.10

WASHING POLISHED AREAS, INTERNALLY AND VIAS WITH PRESSURE JETS, IP-0006, 3.10

	12
	T56A	INSPEÇÃO / INSPECTION	INSPEÇÃO FINAL.
FINAL INSPECTION.
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· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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