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	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	Serviço PrincipaL
(Main Service)
	QUANT:

	CAE-550367
	           AIR INLET HOUSING
	REVISÃO GERAL / OVERHAUL	1

	
	
	
	

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	1
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	REMOVER O CAGE DO DIÂMETRO ¨AF¨ E PEDIR PARA O CONTROLE ENTREGAR ANTECIPADO PARA INSPEÇÃO, EM MÃOS.

REMOVE THE CAGE FROM THE DIAMETER ̈AF ̈ AND ASK THE CONTROL TO DELIVER IT IN ADVANCE FOR INSPECTION, BY HAND.

	2
	REPAIR SHOP	SOLDAR / WELDING	PREPARAR E SOLDAR UMA TRINCA ASSINALADA.
AMS 4118
 VEJA A FOTO ANEXA.

PREPARE AND WELD A MARKED CRACK. AMS 4118 SEE THE ATTACHED PHOTO.

	3
	NDT	END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION	EXECUTAR FPI NA ÁREA DA SOLDA.
ASTM E 1417, METHOD-A, LEVEL-3.

PERFORM FPI IN THE WELD AREA. ASTM E 1417, METHOD-A, LEVEL-3.

	4
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10
CLEAR AS PER IP-0006, 3.10

	5
	REPAIR SHOP	ISOLAÇÃO / MASK	ISOLAR AS ROSCAS, DIÂMETROS E ÁREAS DE CONTATO.
ISOLATE THE THREADS, DIAMETERS AND CONTACT AREAS.

	6
	REPAIR SHOP	PINTURA / PAINTING	PINTAR COM PRIMER PA-0060 e APÓS COM CINZA PA-0065.

PAINT WITH PRIMER PA-0060 and THEN WITH GRAY PA-0065.

	7
	REPAIR SHOP	REMOVER ISOLAMENTO / REMOVE MASK	REMOVER AS ISOLAÇÕES E OS EXCESSOS DE TINTA.

REMOVE INSULATION AND EXCESS PAINT.

	8
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	INSTALAR O CAGE E FRENA-LO COM 2- PINOS P/N= MS9105-53

INSTALL THE CAGE AND BRAKE IT WITH 2-PIN P/N= MS9105-53

	9
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	REMOVER O ANEL DO DIÂMETRO ¨AD¨ e INSTALAR O NOVO P/N= 23039711

REMOVE THE RING FROM THE DIAMETER ̈AD ̈ AND INSTALL THE NEW P/N= 23039711

	10
	REPAIR SHOP	USINAGEM / MACHINING	USINAR O ANEL MAIOR, CENTRANDO PELO DIÂMETRO INTERNO DO PRÓPRIO:
DEIXAR A ALTURA= 0.159¨+ou- 0.002¨
DEIXAR O DIA INTERNO= 15.091¨+ 0.002¨
DEIXAR O DIA EXTERNO= 15.3462¨+ou- 0.0002¨
VEJA AS FIGURAS ANEXAS.

MACHINING THE LARGER RING, CENTERING BY THE INNER DIAMETER OF THE RING ITSELF: LEAVE HEIGHT= 0.159 ̈+or- 0.002 ̈ LEAVE THE DAY INDOORS= 15.091 ̈ + 0.002 ̈ LEAVE DAY OUTSIDE= 15.3462 ̈+or- 0.0002 ̈ SEE THE ATTACHED FIGURES.

	11
	REPAIR SHOP	RETIFICA / RECTIFY	RETIFICAR O DIÂMETRO INTERNO DO CAGE, DEIXANDO= 4.3341¨+ou- 0.0002¨, CENTRADO PELO ANEL GRANDE.

RECTIFY THE INNER DIAMETER OF THE CAGE, LETTING= 4.3341 ̈+or- 0.0002 ̈, CENTERED BY THE LARGE RING.

	12
	REPAIR SHOP	PINTURA / PAINTING	ISOLAR E APLICAR EMBORRACHAMENTO NO BORDO DE ATAQUE DOS STRUTS.

ISOLATE AND APPLY RUBBER COATING TO THE LEADING EDGE OF THE STRUTS.

	13
	T56A	INSPEÇÃO / INSPECTION	INSPEÇÃO FINAL.
(  )APROVADO     (  )REPROVADO

FINAL INSPECTION. ( )APPROVED ( )FAILED

	OBSERVAÇÕES
(Observation):
	ASSINATURA DO SOLICITANTE 
(Signature):
	DATA 12/05/2026
(Date):

	[bookmark: Texto2]     
	VILSON BARBOSA
	12/05/2026


· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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