| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN: 02623 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6848669 |  |  | XX134375 |  |  |  |  | 052062 |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| CAE-550367 |  |  |  | AIR INLET HOUSING |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | REMOVER O CAGE DO DIÂMETRO ¨AF¨ E PEDIR PARA O CONTROLE ENTREGAR ANTECIPADO PARA INSPEÇÃO, EM MÃOS. REMOVE THE CAGE FROM THE DIAMETER ̈AF ̈ AND ASK THE CONTROL TO DELIVER IT IN ADVANCE FOR INSPECTION, BY HAND. |  |  |  |  |  |  |
| 2 | REPAIR SHOP | SOLDAR / WELDING |  |  | PREPARAR E SOLDAR UMA TRINCA ASSINALADA. AMS 4118 VEJA A FOTO ANEXA. PREPARE AND WELD A MARKED CRACK. AMS 4118 SEE THE ATTACHED PHOTO. |  |  |  |  |  |  |
| 3 | NDT | END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION |  |  | EXECUTAR FPI NA ÁREA DA SOLDA. ASTM E 1417, METHOD-A, LEVEL-3. PERFORM FPI IN THE WELD AREA. ASTM E 1417, METHOD-A, LEVEL-3. |  |  |  |  |  |  |
| 4 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 5 | REPAIR SHOP | ISOLAÇÃO / MASK |  |  | ISOLAR AS ROSCAS, DIÂMETROS E ÁREAS DE CONTATO. ISOLATE THE THREADS, DIAMETERS AND CONTACT AREAS. |  |  |  |  |  |  |
| 6 | REPAIR SHOP | PINTURA / PAINTING |  |  | PINTAR COM PRIMER PA-0060 e APÓS COM CINZA PA-0065. PAINT WITH PRIMER PA-0060 and THEN WITH GRAY PA-0065. |  |  |  |  |  |  |
| 7 | REPAIR SHOP | REMOVER ISOLAMENTO / REMOVE MASK |  |  | REMOVER AS ISOLAÇÕES E OS EXCESSOS DE TINTA. REMOVE INSULATION AND EXCESS PAINT. |  |  |  |  |  |  |
| 8 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | INSTALAR O CAGE E FRENA-LO COM 2- PINOS P/N= MS9105-53 INSTALL THE CAGE AND BRAKE IT WITH 2-PIN P/N= MS9105-53 |  |  |  |  |  |  |
| 9 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | REMOVER O ANEL DO DIÂMETRO ¨AD¨ e INSTALAR O NOVO P/N= 23039711 REMOVE THE RING FROM THE DIAMETER ̈AD ̈ AND INSTALL THE NEW P/N= 23039711 |  |  |  |  |  |  |
| 10 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR O ANEL MAIOR, CENTRANDO PELO DIÂMETRO INTERNO DO PRÓPRIO: DEIXAR A ALTURA= 0.159¨+ou- 0.002¨ DEIXAR O DIA INTERNO= 15.091¨+ 0.002¨ DEIXAR O DIA EXTERNO= 15.3462¨+ou- 0.0002¨ VEJA AS FIGURAS ANEXAS. MACHINING THE LARGER RING, CENTERING BY THE INNER DIAMETER OF THE RING ITSELF: LEAVE HEIGHT= 0.159 ̈+or- 0.002 ̈ LEAVE THE DAY INDOORS= 15.091 ̈ + 0.002 ̈ LEAVE DAY OUTSIDE= 15.3462 ̈+or- 0.0002 ̈ SEE THE ATTACHED FIGURES. |  |  |  |  |  |  |
| 11 | REPAIR SHOP | RETIFICA / RECTIFY |  |  | RETIFICAR O DIÂMETRO INTERNO DO CAGE, DEIXANDO= 4.3341¨+ou- 0.0002¨, CENTRADO PELO ANEL GRANDE. RECTIFY THE INNER DIAMETER OF THE CAGE, LETTING= 4.3341 ̈+or- 0.0002 ̈, CENTERED BY THE LARGE RING. |  |  |  |  |  |  |
| 12 | REPAIR SHOP | PINTURA / PAINTING |  |  | ISOLAR E APLICAR EMBORRACHAMENTO NO BORDO DE ATAQUE DOS STRUTS. ISOLATE AND APPLY RUBBER COATING TO THE LEADING EDGE OF THE STRUTS. |  |  |  |  |  |  |
| 13 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 12/05/2026 (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 12/05/2026 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)