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	REGISTRO
	REVISÃO
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	RECORD
	REVISION
	

	CODIGO | CODE
	SOLICITAÇÃO DE SERVIÇOS COMPLEMENTARES
	PÁGINA
	1/1

	IAS-RG-0103
	SUPPLEMENTARY REQUEST
	PAGE
	



	PN (PN):
	SN:
	Nº da OS (WO):
	TLN: 01153

	            6859604
	                  0494926
	050700
	

	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	Serviço PrincipaL
(Main Service)
	QUANT:

	COMPRESSOR- ADOC 702131- EQUADOR
	1- VANE 4º ST
	REVISÃO GERAL / OVERHAUL	1

	
	
	
	

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	1
	REPAIR SHOP	DESAMASSAR / SMOOTH OUT	DESAMASSAR AS ÁREAS ASSINALADAS NAS ALHETAS.

UNDENT THE AREAS MARKED ON THE FINS.

	2
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	SUAVISAR OS PIQUES NAS BORDAS DAS ALHETAS.

SMOOTH THE PIKES ON THE EDGES OF THE FINS.

	3
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	
REAPERTAR A PONTA DAS 10- ALHETAS JUNTO AO OUTER BAND, ADJACENTE AOS FUROS.
RETIGHTEN THE TIP OF THE 10-FLAPS NEXT TO THE OUTER BAND, ADJACENT TO THE HOLES.

	4
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.8
CLEAR AS PER IP-0006, 3.8

	5
	NDT	END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION	EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL 3.
APRESENTOU INDICAÇÃO? ( )SIM        ( )NÃO
RUN FPI: ASTM E 1417, METHOD-A, LEVEL 3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	6
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	7
	CHEMICAL CLEANING	DEPOSIÇÃO DE NIQUEL-CADMIO / NICKEL-CADMIUM PLATING	APLICAR BANHO DE NICKEL CÁDMIO, CONFORME AMS 2416.
APPLY NICKEL CADMIUM BATH, ACCORDING TO AMS 2416.

	8
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	MONTAR OS CORRUGADOS CONFORME A IT-0051.
ASSEMBLE THE CORRUGATED PRODUCTS ACCORDING TO IT-0051.

	9
	T56A	INSPEÇÃO / INSPECTION	INSPEÇÃO FINAL.
 ( )APROVADO      ( )REPROVADO
FINAL INSPECTION. ( )APPROVED ( )FAILED

	
	Escolher um item.	Escolher um item.	

	
	
	
	

	OBSERVAÇÕES
(Observation):
	ASSINATURA DO SOLICITANTE 
(Signature):
	DATA 03/06/2026
(Date):

	[bookmark: Texto2]     
	VILSON BARBOSA
	03/06/2026


· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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