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	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
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	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	1
	REPAIR SHOP	SOLDAR / WELDING	REMOVER 1- PEDAÇO DE PARAFUSO NA LATERAL EXTERNA E LIMPAR A ROSCA ONDE ESTAVA.

REMOVE 1- PIECE OF SCREW ON THE OUTER SIDE AND CLEAN THE THREAD WHERE IT WAS.

	2
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	APLICAR 1- HELICOIL NA MESMA FACE, QUE FOI REMOVIDO PEDAÇO DE PARAFUSO.

APPLY 1- HELICOIL ON THE SAME FACE, WHICH HAS REMOVED PIECE OF SCREW.

	3
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPEZA ALCALINA INTERNA E EXTERNA, IP-0006, 3.8

INTERNAL AND EXTERNAL ALKALINE CLEANING, IP-0006, 3.8

	4
	NDT	END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION	EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL-3.
APRESENTOU INDICAÇÃO?  ( )SIM     ( )NÃO
RUN FPI: ASTM E 1417, METHOD-A, LEVEL-3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	5
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10
 INCLUSIVE COM PRESSÃO NAS LINHAS.
CLEAR AS PER IP-0006, 3.10 EVEN WITH PRESSURE ON THE LINES.

	6
	REPAIR SHOP	SOLDAR / WELDING	INSTALAR A BAFFLE P/N=6874445 COM PONTOS DE SOLDA, NO INTERIOR DA ÁREA CÔNICA.
INSTALL THE BAFFLE P/N=6874445 WITH WELDING POINTS, INSIDE THE CONICAL AREA.

	7
	REPAIR SHOP	ISOLAÇÃO / MASK	ISOLAR OS PRISIONEIROS, OS FUROS COM E SEM ROSCA, DIÂMETRO PILOT E AS FACES DE CONTATO.
ISOLATE STUDS, THREADED AND THREADED HOLES, PILOT DIAMETER AND CONTACT FACES.

	8
	REPAIR SHOP	PINTURA / PAINTING	APLICAR EXTERNAMENTE UMA CAMADA DE SERMETEL, CONFORME A IP-0006, 3.17
APPLY A LAYER OF SERMETEL EXTERNALLY, ACCORDING TO IP-0006, 3.17

	9
	REPAIR SHOP	REMOVER ISOLAMENTO / REMOVE MASK	REMOVER AS ISOLAÇÕES E OS EXCESOS DE SERMETEL.
REMOVE THE INSULATION AND EXCESS OF SERMETEL.

	10
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	                  REMOVER OS PINOS DO SLEEVE E O MESMO.
LIMPAR COM LIXA OU ESCOVA AS ÁREAS DE CONTATO
E REINSTALAR O SLEEVE COM NOVO SELANTE.
                       NOTA: NÃO FRENAR ANTES DO TESTE DE PRESSÃO.

REMOVING THE PINS FROM THE SLEEVE IS THE SAME. CLEAN CONTACT AREAS WITH SANDPAPER OR BRUSH AND REINSTALL THE SLEEVE WITH NEW SEALANT. NOTE: DO NOT BRAKE BEFORE THE PRESSURE TEST.

	11
	T56A	INSPEÇÃO / INSPECTION	TESTE DE PRESSÃO.

PRESSURE TEST.

	12
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	FRENAR O SLEEVE COM 2- PINOS P/N=6739977.

POLISH ALL THREADS AND CONTACT AREAS.

	POLISH ALL THREADS AND CONTACT AREAS. 13
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	POLIR TODAS AS ROSCAS E ÁREAS DE CONTATO.

POLISH ALL THREADS AND CONTACT AREAS.

	14
	T56A	INSPEÇÃO / INSPECTION	INSPEÇÃO FINAL.
( )APROVADO      ( )REPROVADO

FINAL INSPECTION. ( )APPROVED ( )FAILED

	OBSERVAÇÕES
(Observation):
	ASSINATURA DO SOLICITANTE 
(Signature):
	DATA 08/06/2026
(Date):
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	VILSON BARBOSA
	08/06/2026


· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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