| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN: 01153 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6876496 |  |  | 25331 |  |  |  |  | 050700 |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| COMPRESSOR- ADOC 702131- EQUADOR |  |  |  | DIFFUSER |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | REPAIR SHOP | SOLDAR / WELDING |  |  | REMOVER 1- PEDAÇO DE PARAFUSO NA LATERAL EXTERNA E LIMPAR A ROSCA ONDE ESTAVA. REMOVE 1- PIECE OF SCREW ON THE OUTER SIDE AND CLEAN THE THREAD WHERE IT WAS. |  |  |  |  |  |  |
| 2 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | APLICAR 1- HELICOIL NA MESMA FACE, QUE FOI REMOVIDO PEDAÇO DE PARAFUSO. APPLY 1- HELICOIL ON THE SAME FACE, WHICH HAS REMOVED PIECE OF SCREW. |  |  |  |  |  |  |
| 3 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPEZA ALCALINA INTERNA E EXTERNA, IP-0006, 3.8 INTERNAL AND EXTERNAL ALKALINE CLEANING, IP-0006, 3.8 |  |  |  |  |  |  |
| 4 | NDT | END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION |  |  | EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL-3. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN FPI: ASTM E 1417, METHOD-A, LEVEL-3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 5 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 INCLUSIVE COM PRESSÃO NAS LINHAS. CLEAR AS PER IP-0006, 3.10 EVEN WITH PRESSURE ON THE LINES. |  |  |  |  |  |  |
| 6 | REPAIR SHOP | SOLDAR / WELDING |  |  | INSTALAR A BAFFLE P/N=6874445 COM PONTOS DE SOLDA, NO INTERIOR DA ÁREA CÔNICA. INSTALL THE BAFFLE P/N=6874445 WITH WELDING POINTS, INSIDE THE CONICAL AREA. |  |  |  |  |  |  |
| 7 | REPAIR SHOP | ISOLAÇÃO / MASK |  |  | ISOLAR OS PRISIONEIROS, OS FUROS COM E SEM ROSCA, DIÂMETRO PILOT E AS FACES DE CONTATO. ISOLATE STUDS, THREADED AND THREADED HOLES, PILOT DIAMETER AND CONTACT FACES. |  |  |  |  |  |  |
| 8 | REPAIR SHOP | PINTURA / PAINTING |  |  | APLICAR EXTERNAMENTE UMA CAMADA DE SERMETEL, CONFORME A IP-0006, 3.17 APPLY A LAYER OF SERMETEL EXTERNALLY, ACCORDING TO IP-0006, 3.17 |  |  |  |  |  |  |
| 9 | REPAIR SHOP | REMOVER ISOLAMENTO / REMOVE MASK |  |  | REMOVER AS ISOLAÇÕES E OS EXCESOS DE SERMETEL. REMOVE THE INSULATION AND EXCESS OF SERMETEL. |  |  |  |  |  |  |
| 10 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | REMOVER OS PINOS DO SLEEVE E O MESMO. LIMPAR COM LIXA OU ESCOVA AS ÁREAS DE CONTATO E REINSTALAR O SLEEVE COM NOVO SELANTE. NOTA: NÃO FRENAR ANTES DO TESTE DE PRESSÃO. REMOVING THE PINS FROM THE SLEEVE IS THE SAME. CLEAN CONTACT AREAS WITH SANDPAPER OR BRUSH AND REINSTALL THE SLEEVE WITH NEW SEALANT. NOTE: DO NOT BRAKE BEFORE THE PRESSURE TEST. |  |  |  |  |  |  |
| 11 | T56A | INSPEÇÃO / INSPECTION |  |  | TESTE DE PRESSÃO. PRESSURE TEST. |  |  |  |  |  |  |
| 12 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | FRENAR O SLEEVE COM 2- PINOS P/N=6739977. POLISH ALL THREADS AND CONTACT AREAS. |  |  |  |  |  |  |
| POLISH ALL THREADS AND CONTACT AREAS. 13 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | POLIR TODAS AS ROSCAS E ÁREAS DE CONTATO. POLISH ALL THREADS AND CONTACT AREAS. |  |  |  |  |  |  |
| 14 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 08/06/2026 (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 08/06/2026 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)