| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN: 01153 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6848669 |  |  | XX15568 |  |  |  |  | 050700 |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| COMPRESSOR- ADOC 702131- EQUADOR |  |  |  | AIR INLET HOUSING |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | REMOVER O CAGE CENTRAL. NOTA: PEDIR PARA O CONTROLE ENTREGAR DE IMEDIATO O CAGE EM MÃOS PARA A INSPEÇÃO. REMOVE THE CENTER CAGE. NOTE: ASK THE CONTROL TO IMMEDIATELY HAND OVER THE CAGE FOR INSPECTION. |  |  |  |  |  |  |
| 2 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 3 | NDT | END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION |  |  | EXECUTAR FPI: ASTM E 1417. METHOD-A, LEVEL-3. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN FPI: ASTM AND 1417. METHOD-A, LEVEL-3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 4 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 5 | REPAIR SHOP | ISOLAÇÃO / MASK |  |  | ISOLAR OS PRISIONEIROS, OS FUROS E AS ÁREAS DE CONBTATO. ISOLATE PRISONERS, HOLES AND AREAS OF CONTACT. |  |  |  |  |  |  |
| 6 | REPAIR SHOP | PINTURA / PAINTING |  |  | PINTAR EXTERNAMENTE COM: PRIME PA-0060 e CINZA PA-0065. PAINT EXTERNALLY WITH: PRIME PA-0060 and GRAY PA-0065. |  |  |  |  |  |  |
| 7 | REPAIR SHOP | REMOVER ISOLAMENTO / REMOVE MASK |  |  | REMOVER AS ISOLAÇÕES E OS EXCESSOS DE TINTA. REMOVE INSULATION AND EXCESS PAINT. |  |  |  |  |  |  |
| 8 | REPAIR SHOP | ISOLAÇÃO / MASK |  |  | ISOLAR O NECESSÁRIO PARA APLICAR EMBORRACHAMENTO NO BORDO DE ATAQUE DOS STRUTS. ISOLATE WHAT IS NECESSARY TO APPLY RUBBERIZING TO THE LEADING EDGE OF THE STRUTS. |  |  |  |  |  |  |
| 9 | REPAIR SHOP | PINTURA / PAINTING |  |  | APLICAR EMBORRACHAMENTO NO BORDO DE ATAQUE DOS STRUTS. APPLY RUBBER TO THE LEADING EDGE OF THE STRUTS. |  |  |  |  |  |  |
| 10 | REPAIR SHOP | REMOVER ISOLAMENTO / REMOVE MASK |  |  | REMOVER AS ISOLAÇÕES E OS EXCESSOS. REMOVE INSULATION AND EXCESSES. |  |  |  |  |  |  |
| 11 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | MONTAR O CAGE E FRENA-LO COM 2- PINOS P/N=MS9105-53 MONTAR O CAGE E FRENA-LO COM 2- PINOS P/N=MS9105-53 |  |  |  |  |  |  |
| 12 | REPAIR SHOP | RETIFICA / RECTIFY |  |  | RETIFICAR O DIÂMETRO INTERNO DO CAGE, DEIXANDO COM 4.3341¨+ou-0.0002¨ RECTIFY THE INNER DIAMETER OF THE CAGE, LEAVING IT WITH 4.3341 ̈+or-0.0002 |  |  |  |  |  |  |
| 13 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 09/06/2026 (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 09/06/2026 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)