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	PN (PN):
	SN:
	Nº da OS (WO):
	TLN: 01153

	                   6848669
	                        XX15568
	050700
	

	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	Serviço PrincipaL
(Main Service)
	QUANT:

	COMPRESSOR- ADOC 702131- EQUADOR
	          AIR INLET HOUSING
	REVISÃO GERAL / OVERHAUL	1

	
	
	
	

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	1
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	REMOVER O CAGE CENTRAL.
                   NOTA: PEDIR PARA O CONTROLE ENTREGAR DE IMEDIATO O CAGE EM MÃOS PARA A INSPEÇÃO.

REMOVE THE CENTER CAGE. NOTE: ASK THE CONTROL TO IMMEDIATELY HAND OVER THE CAGE FOR INSPECTION.

	2
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	3
	NDT	END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION	EXECUTAR FPI: ASTM E 1417. METHOD-A, LEVEL-3.
APRESENTOU INDICAÇÃO? ( )SIM       ( )NÃO
RUN FPI: ASTM AND 1417. METHOD-A, LEVEL-3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	4
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	5
	REPAIR SHOP	ISOLAÇÃO / MASK	ISOLAR OS PRISIONEIROS, OS FUROS E AS ÁREAS DE CONBTATO.

ISOLATE PRISONERS, HOLES AND AREAS OF CONTACT.

	6
	REPAIR SHOP	PINTURA / PAINTING	PINTAR EXTERNAMENTE COM:
PRIME PA-0060 e CINZA PA-0065.

PAINT EXTERNALLY WITH: PRIME PA-0060 and GRAY PA-0065.

	7
	REPAIR SHOP	REMOVER ISOLAMENTO / REMOVE MASK	REMOVER AS ISOLAÇÕES E OS EXCESSOS DE TINTA.
REMOVE INSULATION AND EXCESS PAINT.

	8
	REPAIR SHOP	ISOLAÇÃO / MASK	ISOLAR O NECESSÁRIO PARA APLICAR EMBORRACHAMENTO NO BORDO DE ATAQUE DOS STRUTS.
ISOLATE WHAT IS NECESSARY TO APPLY RUBBERIZING TO THE LEADING EDGE OF THE STRUTS.

	9
	REPAIR SHOP	PINTURA / PAINTING	APLICAR EMBORRACHAMENTO NO BORDO DE ATAQUE DOS STRUTS.

APPLY RUBBER TO THE LEADING EDGE OF THE STRUTS.

	10
	REPAIR SHOP	REMOVER ISOLAMENTO / REMOVE MASK	REMOVER AS ISOLAÇÕES E OS EXCESSOS.

REMOVE INSULATION AND EXCESSES.

	11
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	MONTAR O CAGE E FRENA-LO COM 2- PINOS P/N=MS9105-53

MONTAR O CAGE E FRENA-LO COM 2- PINOS P/N=MS9105-53

	12
	REPAIR SHOP	RETIFICA / RECTIFY	RETIFICAR O DIÂMETRO INTERNO DO CAGE, DEIXANDO COM 4.3341¨+ou-0.0002¨

RECTIFY THE INNER DIAMETER OF THE CAGE, LEAVING IT WITH 4.3341 ̈+or-0.0002

	13
	T56A	INSPEÇÃO / INSPECTION	INSPEÇÃO FINAL.
( )APROVADO        ( )REPROVADO

FINAL INSPECTION. ( )APPROVED ( )FAILED

	
	Escolher um item.	Escolher um item.	

	
	Escolher um item.	Escolher um item.	

	
	Escolher um item.	Escolher um item.	

	OBSERVAÇÕES
(Observation):
	ASSINATURA DO SOLICITANTE 
(Signature):
	DATA 09/06/2026
(Date):

	[bookmark: Texto2]     
	VILSON BARBOSA
	09/06/2026


· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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