| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN: 02188 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6871447 |  |  | 6012 |  |  |  |  | 050700 |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| ADOC702131 |  |  |  | COMPRESSOR CASE |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR OS 14- DIÂMETROS INTERNOS ATÉ REMOVER TODO MATERIAL BASE. MACHINE THE 14- INTERNAL DIAMETERS UNTIL ALL BASE MATERIAL IS REMOVED. |  |  |  |  |  |  |
|  | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR O DIÂMETRO INTERNO ¨Q¨, DEIXANDO= 15.368¨+0.002¨ CENTRANDO COM O DIÂMETRO INTERNO QUE ALOJA A PRIMEIRA VANE. VEJA A FIGURA ANEXA. MACHINING THE INNER DIAMETER ̈Q ̈, LEAVING= 15.368 ̈+0.002 ̈ CENTERING WITH THE INNER DIAMETER HOUSING THE FIRST VANE. SEE THE ATTACHED FIGURE. |  |  |  |  |  |  |
| 2 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | REMOVER OS PARAFUSOS DE UNIÃO , PARA SEPARAR EM 2- METADES. MANTER OS PARAFUSOS COM O CARTER. REMOVE THE BOLTS OF UNION, TO SEPARATE INTO 2-HALVES. |  |  |  |  |  |  |
| 3 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 4 | NDT | END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION |  |  | EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL-3. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN FPI: ASTM E 1417, METHOD-A, LEVEL-3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 5 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
|  | REPAIR SHOP | ISOLAÇÃO / MASK |  |  | ISOLAR OS FUROS, ROSCAS, INTERNAMENTE E AS ÁREAS DE CONTATO. ISOLATE THE HOLES, THREADS, INTERNALS AND CONTACT AREAS. |  |  |  |  |  |  |
| 6 | REPAIR SHOP | PINTURA / PAINTING |  |  | APLICAR EXTERNAMENTE SERMETEL W ou ALSEAL 500., IP-0006, 3.17 APPLY EXTERNALLY SERMETEL 518, IP-0006, 3.17 |  |  |  |  |  |  |
|  | REPAIR SHOP | REMOVER ISOLAMENTO / REMOVE MASK |  |  | REMOVER AS ISOLAÇÕES E OS EXCESSOS DE SERMETEL. REMOVE INSULATION AND EXCESS FROM SERMETEL. |  |  |  |  |  |  |
|  | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | LIMPAR AS FACES E UNIR AS 2- METADES, COM 9- PARAFUSOS DE CADA LADO. CLEAN THE FACES AND JOIN THE 2- HALVES, WITH 9- SCREWS ON EACH SIDE. |  |  |  |  |  |  |
|  | REPAIR SHOP | METALIZAÇÃO / THERMAL SPRAY |  |  | ISOLAR E METALIZAR O DIÂMETRO PILOT- ¨Q¨ COM METCO 444. INSULATE AND METALLIZE THE PILOT- ̈Q ̈ DIAMETER WITH HAMMER 444. |  |  |  |  |  |  |
| 7 | REPAIR SHOP | METALIZAÇÃO / THERMAL SPRAY |  |  | ISOLAR E METALIZAR INTERNAMENTE COM ALUMÍNIO. INTERNALLY METALLIZE WITH ALUMINUM. |  |  |  |  |  |  |
| 8 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR O DIÂMETRO ¨Q¨METALIZADO, DEIXANDO CENTRADO COM O DIÂMETRO INTERNO QUE ALOJA A VANE DO PRIMEIRO ESTÁGIO E COM 15.347¨+ou- 0.001¨ VEJA A FIGURA 1- ANEXA. |  |  |  |  |  |  |
| 9 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR AS CANALETAS, REMOVENDO O ALUMÍNIO E DEIXANDO NAS MEDIDAS DA FIGURA DA PÁGINA-924 ANEXA. MACHINE THE GUTTERS, REMOVING THE ALUMINUM AND LEAVING IT IN THE MEASUREMENTS OF THE FIGURE ON PAGE-924 ATTACHED. |  |  |  |  |  |  |
| 10 | REPAIR SHOP | USINAGEM / MACHINING |  |  | CENTRAR PELOS DIÂMETROS INTERNOS, QUE ALOJAM AS VANES DAS EXTREMIDADES. USINAR O DIÂMETRO DOS 14- RESALTOS INTERNOS, DEIXANDO: DO 1º ao 9º ST= 14. 729¨ +ou- 0.001¨ e DO 10º ao 14º ST= 14.735¨+ou- 0.001¨ VEJA A FIGURA DA PÁGINA 923 ANEXA. |  |  |  |  |  |  |
| 11 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR OS 3- TIPOS DE CHANFROS, CONFORME AS MEDIDAS DA FIGURA DA PÁGINA 923 ANEXA. MACHINE THE 3- TYPES OF CHAMFERS, ACCORDING TO THE MEASUREMENTS OF THE FIGURE ON PAGE 923 ATTACHED. |  |  |  |  |  |  |
| 12 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | SUAVISAR AS ÁREAS USINADAS, REMOVENDO OS EXCESSOS DE ALUMÍNIO. SMOOTH THE MACHINED AREAS, REMOVING EXCESS ALUMINUM. |  |  |  |  |  |  |
| 13 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | LIMPAR E POLIR AS ROSCAS E FACES DE CONTATO. CLEAN AND POLISH THE THREADS AND CONTACT FACES. |  |  |  |  |  |  |
| 14 | T56A | MONTAG EM/ ASSEMBLY |  |  | MONTAR AS VANES, CONFORME AS MEDIDAS DA PÁGINA 924 ANEXA. ASSEMBLE THE VANES, ACCORDING TO THE MEASUREMENTS ON PAGE 924 ATTACHED. |  |  |  |  |  |  |
| 15 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | AJUSTAR AS PONTAS DOS ARCOS DA VANES, REMOVENTO O QUE EXCEDER DAS FACES DAS METADES. ADJUST THE TIPS OF THE VANES ARCHES, REMOVING WHAT EXCEEDS THE FACES OF THE HALVES. |  |  |  |  |  |  |
| 16 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | LIMPAR AS FACES E UNIR AS 2- METADES COM VÁRIOS PARAFUSOS. CLEAN THE FACES AND JOIN THE 2- HALVES WITH SEVERAL SCREWS. |  |  |  |  |  |  |
| 17 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR OS DIÂMETROS INTERNOS DOS SEALS DAS VANES, CONFORME A TABELA DA PÁGINA 405 ANEXA. MACHINE THE INTERNAL DIAMETERS OF THE SEALS OF THE VANES, ACCORDING TO THE TABLE ON PAGE 405 ATTACHED. |  |  |  |  |  |  |
| 18 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LAVAR CONFORME A IP-0006, 3.10 WASH ACCORDING TO IP-0006, 3.10 |  |  |  |  |  |  |
| 19 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( ) APROVADO ( )REPROVADO FINAL INSPECTION. ( ) APPROVED ( )FAILED |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 10/06/2026 (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 10/06/2026 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)