| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN: 01153 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6858624 |  |  | KK25239 |  |  |  |  | 050700 |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| COMPRESSOR- ADOC 702131- EQUADOR |  |  |  | WHEEL 14º ST |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | REMOVER TODOS PEDAÇOS DE PINOS. REMOVE ALL PIECES OF PINS. |  |  |  |  |  |  |
| 2 | REPAIR SHOP | JATEAR / BLAST |  |  | ISOLAR E EXECUTAR SHOT PEEN NA FACE TRASEIRA, CONFORME AS INSTRUÇÕES DO WP 147 00, PÁGINAS 20 e 21 ANEXAS. VEJA A FIGURA ANEXA. ISOLATE AND PERFORM SHOT PEEN ON THE REAR FACE, AS INSTRUCTED IN WP 147 00, PAGES 20 and 21 ANNEXED. SEE THE ATTACHED FIGURE. |  |  |  |  |  |  |
| 3 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO DIMENCIONAL DO DISH. DIMENSIONAL DISH INSPECTION. |  |  |  |  |  |  |
| 4 | CHEMICAL CLEANING | DEPOSIÇÃO DE PRATA/ SILVER PLATING |  |  | ISOLAR E APLICAR BANHO DE PRATA (AMS 2410) NA ROSCA INTERNA. ISOLATE AND APPLY SILVER PLATING (AMS 2410) ON THE INTERNAL THREAD. |  |  |  |  |  |  |
| 5 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 6 | NDT | END- PARTICULAS MAGNETICAS / NOT - MAGNETIC PARTICLE |  |  | EXECUTAR MPI: ASTM E 1444. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN MPI: ASTM E 1444. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 7 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 8 | NDT | END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION |  |  | EXECUTAR FPI: ASTM E 1417, METHOD-D, LEVEL-4. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN FPI: ASTM E 1417, METHOD-D, LEVEL-4. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 9 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 10 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | INSTALAR AS PALHETAS E FRENA-LAS COM PINOS P/N= 6731108 INSTALL THE BLADES AND BRAKE THEM WITH P/N PINS = 6731108 |  |  |  |  |  |  |
| 11 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 10/06/2026 (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 10/06/2026 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)