| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN: 01153 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 23055560 |  |  | WY72402 |  |  |  |  | 050700 |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| AD0C702131 |  |  |  | WHEEL 10º ST |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | REMOVER OS RESQUÍCIOS DE PINOS DOS FUROS DE FRENAGEM. REMOVE ALL REMNANTS OF THE PINS FROM THE LOCKWIRE HOLES |  |  |  |  |  |  |
| 2 | CHEMICAL CLEANING | JATEAR / BLAST |  |  | APLICAR GLASS BEAD NAS ÁREAS ESCURAS INTERNAS DOS ENCAIXES DAS PALHETAS. IP-0006, 3.26 APPLY GLASS BEAD TO THE DARK AREAS INSIDE THE REED FITTINGS. IP-0006, 3.26 |  |  |  |  |  |  |
| 3 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 4 | NDT | END- PARTICULAS MAGNETICAS / NOT - MAGNETIC PARTICLE |  |  | EXECUTAR MPI: ASTM E 1444. APRESENTOU INDICAÇÃO? ( ) SIM ( ) NÃO RUN MPI: ASTM E 1444. DID YOU PRESENT AN INDICATION? ( ) YES ( ) NO |  |  |  |  |  |  |
| 5 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 6 | NDT | END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION |  |  | EXECUTAR FPI: ASTM E 1417, METHOD-D, LEVEL 4. APRESENTOU INDICAÇÕES? ( )SIM ( )NÃO RUN FPI: ASTM E 1417, METHOD-D, LEVEL 4. DID YOU PRESENT INDICATIONS? ( )YES ( )NO |  |  |  |  |  |  |
| 7 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 8 | CHEMICAL CLEANING | DEPOSIÇÃO DE NIQUEL-CADMIO / NICKEL-CADMIUM PLATING |  |  | APLICAR BANHO DE NICKEL CÁDMIO, CONFORME AMS 2416. APPLY NICKEL CADMIUM BATH, ACCORDING TO AMS 2416. |  |  |  |  |  |  |
| 9 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | MONTAR AS PALHETAS. NOTA: Não frena-las. ASSEMBLE THE BLADES. NOTE: Do not brake them. |  |  |  |  |  |  |
| 10 | REPAIR SHOP | BALANCEAMENTO / BALANCING |  |  | BALANCEAR O CONJUNTO. BALANCE THE SET. |  |  |  |  |  |  |
| 11 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | FRENAR AS PALHETAS COM PINOS P/N= 6730907 E EXECUTAR STAK. BRAKE THE VANES WITH PINS P/N= 6730907 AND PERFORM STAK. |  |  |  |  |  |  |
| 12 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 12/06/2026 (Date): |  |
|  |  |  |  |  |  | AUGUSTO ROSA |  |  |  | 12/06/2026 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)