| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN: 02188 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 23006662 |  |  | 15446 |  |  |  |  | IAS |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| T56 - IAS |  |  |  | - PUMP COVER |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | REMOVER A BUCHA DE BRONZE. REMOVE BRONZE BUSHING. |  |  |  |  |  |  |
| 2 | CHEMICAL CLEANING | DECAPAGEM / STRIPPING |  |  | DECAPAR A TINTA, CONFORME A IP-0006, 3.18 INK PICKLING, IN ACCORDANCE WITH IP-0006, 3.18 |  |  |  |  |  |  |
| 3 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 4 | NDT | END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION |  |  | EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL-3. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN FPI: ASTM E 1417, METHOD-A, LEVEL-3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 5 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 6 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | MONTAR A BUCHA E FRENAR COM O PINO P/N= AN150306 VEJA A FIGURA ANEXA. MOUNT THE BUSHING AND BRAKE WITH P/N= AN150306 SEE THE ATTACHED FIGURE. |  |  |  |  |  |  |
| 7 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR O DIÂMETRO INTERNO DA BUCHA, DEIXANDO= 0.5007¨+ou- 0.0002¨ CHANFRAR , DEIXANDO A BUCHA NO MESMO PLANO DA FACE OU LEVEMENTE A BAIXO. VEJA A FIGURA ANEXA. MACHINE THE INNER DIAMETER OF THE BUSHING, LETTING= 0.5007 ̈ + or - 0.0002 ̈ CHAMFER, LEAVING THE ANCHOR IN THE SAME PLANE AS THE FACE OR SLIGHTLY BELOW. SEE THE ATTACHED FIGURE. |  |  |  |  |  |  |
| 8 | REPAIR SHOP | ISOLAÇÃO / MASK |  |  | ISOLAR OS FUROS E A FACE DE CONTATO. ISOLATE THE HOLES AND THE CONTACT FACE. |  |  |  |  |  |  |
| 9 | REPAIR SHOP | PINTURA / PAINTING |  |  | PINTAR EXTERNAMENTE COM: PRIMER PA-0060 e CINZA PA-0065. PAINT EXTERNALLY WITH: PRIMER PA-0060 and GRAY PA-0065. |  |  |  |  |  |  |
| 10 | REPAIR SHOP | REMOVER ISOLAMENTO / REMOVE MASK |  |  | REMOVER AS ISOLAÇÕES E OS EXCESSOS DE TINTA. REMOVE INSULATION AND EXCESS PAINT. |  |  |  |  |  |  |
| 11 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 24/06/2026 (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 24/06/2026 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)