| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN: |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 23076529 |  |  | GK512856 |  |  |  |  | 049650 |  |  | 02124 – 14W3 REV.1 |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| CAT-98301 |  |  |  | TURBINE SPLINE ADAPTER |  |  | REPARO / REPAIR |  | 1 |  |  |
| TSN: |  |  |  | CSN: |  |  | TSO: |  | CSO: |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 01 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | Realizar limpeza desengraxante do item, conforme IAS-IP-0006 item 3.23 para remover todas as impurezas e resquícios de óleo. Perform degreasing cleaning of the item, according to IAS-IP-0006 item 3.23 to remove all impurities and oil remnants. |  |  |  |  |  |  |
| 02 | CHEMICAL CLEANING | DEPOSIÇÃO DE PRATA/ SILVER PLATING |  |  | Restaure banho de prata nas estrias externas com uma espessura de 0,0001-0,0003 pol. (0,003-0,008 mm) (Ref. AMS 2410 ou AMS 2412). Restore the silver plate to the external splines to a thickness of 0.0001-0.0003 in. (0.003-0.008 mm) (Ref. AMS 2410 or AMS 2412). |  |  |  |  |  |  |
| 03 | CHEMICAL CLEANING | TRATAMENTO TERMICO / HEAT TREATMENT |  |  | Realizar aquecimento a 300-500°F e manter essa temperatura por no mínimo 2 horas. Heat to 300-500°F and maintain this temperature for a minimum of 2 hours. |  |  |  |  |  |  |
| 04 | M250 | INSPEÇÃO / INSPECTION |  |  | Realizar inspeção final dos serviços realizados. Perform final inspection of the services performed. |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA (Date): |  |
|  |  |  |  |  |  | MATEUS MACHADO |  |  |  | 25/06/2026 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)