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	REGISTRO
	REVISÃO
	04

	
	RECORD
	REVISION
	

	CODIGO | CODE
	SOLICITAÇÃO DE SERVIÇOS COMPLEMENTARES
	PÁGINA
	1/1

	IAS-RG-0103
	SUPPLEMENTARY REQUEST
	PAGE
	



	PN (PN):
	SN:
	Nº da OS (WO):
	TLN:

	23076529
	GK512856
	049650
	02124 – 14W3 REV.1

	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	Serviço PrincipaL
(Main Service)
	QUANT:

	CAT-98301
	TURBINE SPLINE ADAPTER
	REPARO / REPAIR	1

	TSN:
	CSN:
	TSO:
	CSO:

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	01
	CHEMICAL CLEANING	LIMPAR / CLEAN	Realizar limpeza desengraxante do item, conforme IAS-IP-0006 item 3.23 para remover todas as impurezas e resquícios de óleo. 

Perform degreasing cleaning of the item, according to IAS-IP-0006 item 3.23 to remove all impurities and oil remnants.

	02
	CHEMICAL CLEANING	DEPOSIÇÃO DE PRATA/ SILVER PLATING	Restaure banho de prata nas estrias externas com uma espessura de 0,0001-0,0003 pol.
(0,003-0,008 mm) (Ref. AMS 2410 ou AMS 2412). 

Restore the silver plate to the external splines to a thickness of 0.0001-0.0003 in. (0.003-0.008 mm) (Ref. AMS 2410 or AMS 2412).

	03
	CHEMICAL CLEANING	TRATAMENTO TERMICO / HEAT TREATMENT	Realizar aquecimento a 300-500°F e manter essa temperatura por no mínimo 2 horas.

Heat to 300-500°F and maintain this temperature for a minimum of 2 hours.

	04
	M250	INSPEÇÃO / INSPECTION	Realizar inspeção final dos serviços realizados.

Perform final inspection of the services performed.

	OBSERVAÇÕES
(Observation):
	ASSINATURA DO SOLICITANTE 
(Signature):
	DATA 
(Date):

	[bookmark: Texto2]     
	MATEUS MACHADO
	25/06/2026


· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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