| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN - 02623 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6873732 |  |  | GGK913 |  |  |  |  | 050710 |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| ADOG-033980 |  |  |  | REAR CARRIER BEARING INNER RACE |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | REMOVER AS AGREGAÇÕES DE CROMO DO DIÂMETRO INTERNO E POLIR COM LIXA MÉDIA E FINA. REMOVE THE CHROMIUM AGGREGATIONS FROM THE INNER DIAMETER AND POLISH WITH MEDIUM AND FINE SANDPAPER. |  |  |  |  |  |  |
| 2 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 3 | CHEMICAL CLEANING | DEPOSIÇÃO DE PRATA/ SILVER PLATING |  |  | ISOLAR E APLICAR 0.0008¨DE ESPESSURA DE ¨COBRE¨ NO DIÂMETRO INTERNO. AMS 2400 NOTA-1: MUITO CUIDADO PARA NÃO ATACAR A PISTA EXTERNA POIS É DE ROLAMENTO. NOTA-2: LUBRIFICAR APÓS REMOVER A ISOLAÇÃO. ISOLATE AND APPLY 0.0008 ̈OF COPPER THICKNESS TO THE INNER DIAMETER. AMS 2400 NOTE: BE VERY CAREFUL NOT TO ATTACK THE OUTER TRACK AS IT IS A ROLLING TRACK. |  |  |  |  |  |  |
| 4 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. FINAL INSPECTION. |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 02/07/2026 (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 02/07/2026 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)