| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN: |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| RR30000150 |  |  | YP10283 |  |  |  |  | 055604 |  |  | 02027 |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| CAE-200270 |  |  |  | COVER |  |  | REPARO / REPAIR |  | 01 |  |  |
|  |  |  |  |  |  |  | TSO: |  | CSO: |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 01 | CHEMICAL CLEANING | DECAPAGEM / STRIPPING |  |  | REALIZAR DECAPAGEM DO ITEM CONFORME IAS-IP-0006 3.18 PERFORM PICKLING OF THE ITEM ACCORDING TO IAS-IP-0006 3.18 |  |  |  |  |  |  |
| 02 | NDT | NON-DESTRUCTIVE TESTING |  |  | Realizar NDT no local trabalhado conforme indicado no HMM CSP22005.Perform NDT on reworked area conform indicated in the HMM CSP22005. Ensaio (Test): FPI Tipo (Type): 1 Método (Method): A Sensibilidade (Sensitivity): 2 Foram encontradas indicações? (Were Indications found?) ( ) SIM – REGISTRAR IAS-RG-0332. (YES – REGISTRAR IAS-RG-0332.) ( ) NÃO – PROCESSEGUIR PARA ETAPA DE LIMPEZA PÓS NDT (NO – PROCEED TO THE AFTER NDT CLEANING STEP.) |  |  |  |  |  |  |
| 03 | RR300 | INSPEÇÃO / INSPECTION |  |  | Realizar inspeção pós NDT conforme HMM CSP22005.Perform inspection after NDT i.a.w. HMM CSP22005. Refira-se aos resultados registrados no RG-0332 (se foi feito na etapa anterior) e preencher o mesmo com devidas observações. (Refer to the results registered in the RG-0332 (if it was done in the step before) and fill it in with due observations). Avaliar os limites de aceitação conforme OMM. (Evaluate the acceptance limits conform OMM.) ( ) APROVADO – (APPROVED) ( ) REJEITADO – (REJECTED) |  |  |  |  |  |  |
| 04 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | Realizar limpeza pós NDT conforme IAS-IP-0006 item 3.34 Rev.03. Perform Cleaning post NDT i.a.w. IAS-IP-0006 Item 3.34 Rev.03. |  |  |  |  |  |  |
| 05 | RR300 | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO INSPECTION |  |  |  |  |  |  |
| 06 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | Remover corrosão nas superfícies externas, não aplicar aplicar epoxy nesse momento. . Remove corrosion from external surfaces, do not apply epoxy currently. |  |  |  |  |  |  |
| 07 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | Realizar limpeza da peça conforme IAS-IP-0006 item 3.34 rev.3. Perform Cleaning iaw IAS-IP-0006 item 3.34 rev.3. |  |  |  |  |  |  |
| 08 | CHEMICAL CLEANING | APLICAR / APPLY |  |  | Aplique a solução de dicromato no metal base exposto. Apply the dichromate solution to the bare metal. |  |  |  |  |  |  |
| 09 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | Aplicar EPOXI preenchendo os defeitos causados pela corrozão deixando o perfil mais próximo do original possível. Apply EPOXY filling with the defects caused by corrosion, leaving the profile as close to the original as possible |  |  |  |  |  |  |
| 10 | REPAIR SHOP | PINTURA / PAINTING |  |  | MASCARAMENTO: Isolar os prisioneiros, HELICOILS, faces de assentamento, PN e SN e locais onde não será aplicado coating. (task 70-32-11-300-801 – application of corrosion resistant paint) MASKING: Insolate studs, HELICOILS, seating faces, PN and SN and places where no coating will be applied. (task 70-32-11-300-801 - application of corrosion resistant paint). |  |  |  |  |  |  |
| 11 | REPAIR SHOP | PINTURA / PAINTING |  |  | Realizar pintura conforme IAS-IP-0005 Item 3.13 Rev.05 (task 70-32-11-300-801 – application of corrosion resistant paint). Apply coating per IAS-IP-0005 Item 3.13 Rev.05 (task 70-32-11-300-801 – application of corrosion resistant paint). |  |  |  |  |  |  |
| 12 | CHEMICAL CLEANING | PRESERVAÇÃO / PRESERVATION |  |  | Proteger o componente lubrificando todas as gaiolas de localização dos rolamentos, prisioneiros e inserts. Protect the component by lubricating all bearing location cages, studs and inserts. |  |  |  |  |  |  |
| 13 | RR300 | INSPEÇÃO / INSPECTION |  |  | Inspeção final Final inspection. |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA (Date): |  |
|  |  |  |  |  |  | RICARDO CICALA |  |  |  | 30/07/2026 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)