| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN: 02188 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6850819 |  |  | 14266 |  |  |  |  | IAS |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| IAS / T56 |  |  |  | PRESSURE PUMP BODY |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | REMOVER O SHAFT, POLIR O MESMO PARA ELIMINAR A CORROSÃO E PEDIR PRO CONTROLE LEVAR PARA INSPEÇÃO ENCAMINHAR PARA OXIDAÇÃO NEGRA. REMOVE THE SHAFT, POLISH IT TO ELIMINATE CORROSION AND ASK THE CONTROL TO TAKE IT FOR INSPECTION TO FORWARD IT FOR BLACK OXIDATION. |  |  |  |  |  |  |
| 2 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | ESCOVAR AS ÁREAS COM CORROSÃO: BUCHA, PINOS E PRISIONEIROS. BRUSH THE AREAS WITH CORROSION: BUSHING, PINS AND STUDS. |  |  |  |  |  |  |
| 3 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 4 | CHEMICAL CLEANING | END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION |  |  | EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL-3. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN FPI: ASTM E 1417, METHOD-A, LEVEL-3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 5 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 6 | REPAIR SHOP | ISOLAÇÃO / MASK |  |  | ISOLAR OS PRISIONEIROS, FUROS E AS ÁREAS DE CONTATO. ISOLATE STUDS, HOLES, AND CONTACT AREAS. |  |  |  |  |  |  |
| 7 | REPAIR SHOP | PINTURA / PAINTING |  |  | PINTAR EXTERNAMENTE COM: PRIMER PA-0060 E CINZA PA-0065. PAINT EXTERNALLY WITH: PRIMER PA-0060 AND GRAY PA-0065. |  |  |  |  |  |  |
| 8 | REPAIR SHOP | REMOVER ISOLAMENTO / REMOVE MASK |  |  | REMOVER AS ISOLAÇÕES E OS EXCESSOS DE TINTA. REMOVE INSULATION AND EXCESS PAINT. |  |  |  |  |  |  |
| 9 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | INSTALAR O SHAFT. INSTALL THE SHAFT. |  |  |  |  |  |  |
| 10 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 06/08/2026 (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 06/08/2026 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)