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	CODIGO | CODE
	SOLICITAÇÃO DE SERVIÇOS COMPLEMENTARES
	PÁGINA
	1/1

	IAS-RG-0103
	SUPPLEMENTARY REQUEST
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	PN (PN):
	SN:
	Nº da OS (WO):
	TLN:

	RR30000369
	NC
	051512
	2027

	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	Serviço PrincipaL
(Main Service)
	QUANT:

	RRE-200070/RRT-11069
	SHIELD ASSY, TURBINE NOZZLE, 1ST STAGE
	REPARO / REPAIR	01

	     
	     
	TSO:                    
	CSO:      

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	01
	REPAIR SHOP	SOLDAR / WELDING	Soldar áreas desgastadas das sadlles preenchendo com solda AMS 5839 para recuperar as dimensões conforme Fig. 6 em anexo.

Weld build-up worn area with weld filler material AMS 5839 to get final dimensions as show in Fig. 6 attached.

	02
	REPAIR SHOP	USINAGEM / MACHINING	Usinar faces soldadas das Saddles respeitando as medidas conforme Fig. 6 em anexo.

Machine welded areas to get final dimensions as show in Fig. 6 attached.

	03
	CHEMICAL CLEANING	LIMPAR / CLEAN	Realizar limpeza da peça conforme IAS-IP-0006, 3.34.

Perform Cleaning IAW IAS-IP-0006, 3.34.

	04
	NDT	NON-DESTRUCTIVE TESTING	Realizar NDT LOCAL conforme indicado no (Perform NDT conform indicated in
the.) Overhaul Manual.
Ensaio (Test): FPI
Tipo (Type): 1
Método (Method): A
Sensibilidade (Sensitivity): 2

Foram encontradas indicações?
(Were Indications found?)

( ) SIM – REGISTRAR IAS-RG-0332.
(YES – REGISTRAR IAS-RG-0332.)

( ) NÃO – PROCESSEGUIR PARA ETAPA DE LIMPEZA PÓS NDT
(NO – PROCEED TO THE AFTER NDT CLEANING STEP.)

	05
	RR300	INSPEÇÃO / INSPECTION	Realizar inspeção pós NDT conforme. (Perform inspection after NDT iaw)
Manual.
 Refira-se aos resultados registrados no RG-0332 (se foi feito na etapa
anterior) e preencher o mesmo com devidas observações.

(Refer to the results registered in the RG-0332 (if it was done in the step before) and fill it in with due observations).
 Avaliar os limites de aceitação conforme OMM. (Evaluate the acceptance
limits conform OMM.)

( ) APROVADO – (APPROVED)

( ) REJEITADO – (REJECTED)

	06
	CHEMICAL CLEANING	LIMPAR / CLEAN	Realizar limpeza pós NDT conforme IAS-IP-0006, 3.34.

Perform Cleaning after NDT IAW IAS-IP-0006, 3.34.

	07
	CHEMICAL CLEANING	LIMPAR / CLEAN	Realizar limpeza pós NDT conforme IAS-IP-0006, 3.26.

Perform Cleaning after NDT IAW IAS-IP-0006, 3.26.

	08
	CHEMICAL CLEANING	LIMPAR / CLEAN	Realizar limpeza pós NDT conforme IAS-IP-0006, 3.23.

Perform Cleaning after NDT IAW IAS-IP-0006, 3.23.

	09
	RR300	INSPEÇÃO / INSPECTION	Inspeção final

Final inspection.

	OBSERVAÇÕES
(Observation):
	ASSINATURA DO SOLICITANTE 
(Signature):
	DATA 
(Date):

	[bookmark: Texto2]     
	NATALINO JUNIOR
	25/08/2026


· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)


	




image1.png




